## Slide 1
量測系統示意圖
Probe station
Keithley 2400
Drain-voltage source
Amp amplifier
Drain-current amplify
Keithley 2400
Gate-voltage source
Keithley 2000
Drain-current meter

## Slide 2: 二點探針量測 (Two-probe measurement)
P - Si
N+ - Si
N+ - Si
P - Si
SiO2
Al
Al
Al
Total Resistance = Rtotal = 2Rc + Rs + Rp
Rc = Contact resistance
Rs = Sample(Channel) resistance (P - Si)
Rp = Probe resistance (Probe, Al, N+ - Si)
Rc
Rc
RS
N-type MOSFET
Vdrain = IdrainRtotal
Source
Drain

## Slide 3
MOSFET量測
P - Si
N+ - Si
N+ - Si
P - Si
SiO2
Al
Al
Al
N-type MOSFET
Source
Gate
Drain
P - Si
N+ - Si
N+ - Si
N+ - Si
SiO2
Al
Al
Al
Source
Gate
Drain
After gating

## Slide 4
Flat-band
Vg induce band bending
Strong inversion
( P to N+ )
EF
EC
EV
Semi.
(P - Si)
Oxide
(SiO2)
Metal
(Al)
Vg > 0
Vg > Vth
Oxide (SiO2)
Metal (Al)
Semi.
(P - Si)
Al
Al
N+ - Si
N+ - Si
Oxide (SiO2)
Metal (Al)
Semi.
(P - Si)
Al
Al
N+ - Si
N+ - Si
N+ - Si
Vg > Vth

## Slide 5
https://en.wikipedia.org/wiki/MOSFET

## Slide 7
NMOS
Channel
Source
Drain (positive bias)

## Slide 8
https://www.semanticscholar.org/paper/Revisiting-MOSFET-threshold-voltage-extraction-Ortiz-Conde-Garc%C3%ADa-S%C3%A1nchez/e0fe6cc5e7b7841f16cbb149fd98b6e1179e5057
Carrier mobility = μ = [dID/dVG][L/(WCiVD)]
dID/dVG = Maximum slope
L/W = Channel length/width
VD = Drain voltage
Ci = Capacitance (Ci = ɛ0ɛr/d; ɛr = 3.9; d = 100 nm)
Unit of mobility = cm2 V−1 s−1
Threshold voltage and Carrier mobility
N-type device

## Slide 9
 | Wet Oxide | Ion Implantation | Dry Oxide | Channel length/width
製程參數 | SiO2 : 500 nm | As : 1E15 cm2 / 10 keV B : 1E15 cm2 / 10 kev | SiO2 : 100 nm | 40 μm / 20 μm